Effect of Argon Pressure and Aluminum Content (in TiO2-H3BO3-Al mix)

on Combustion and Formation of Chemical Composition in Combustion

Products

Raimkhanova Danara Serikovna, Fomenko Sergey Mihaylovich, Abdulkarimova Roza Gabdullovna, Mansurov Zulkhair Aimukhametovich

Abstract

Among advanced methods of obtaining the composite materials synthesis in the mode the self-propagating high-temperature synthesis (SHS) is particularly attractive, on account of its advantages of low energy requirement, short processing time, simplicity of facilities, and formation of high-purity products. The SHS technique has been extensively applied to produce a great number of advanced materials such as borides, carbides, nitrides, silicides and intermetallics. SHS method allows obtaining of materials with set properties, which cannot be obtained by conventional methods. At high temperature developing in the course of SHS, some components of the system are transferred to gas for example aluminum. In this case, change of external pressure enables the control over synthesis depth, thus preventing or reducing the loss of volatile system elements and contributing to preservation of main reducing agents in the system. Besides, introduction of slightly excessive aluminum in initial mixtures reduces the effect of evaporation on final product. Possibility of getting the boron-containing composite materials at aluminum-thermal combustion of boron-containing systems in argon medium was shown. The combustion took place in reactor (at up to 30 atm. argon pressure). Influence of argon pressure and aluminum content (in initial feed) on content of the solid (titanium diboride and aluminum oxide) phases in products of self-propagating high-temperature synthesis. Patterns of aluminum-thermal burning (boric acid with titanium oxide) have been set. Dependence between macro-kinetic parameters of SH-synthesis, composition of initial reagents and medium of SH-synthesis has been defined. Based on obtained results, prospects of using the available source components for synthesis of fire-resistant composite materials have been shown.