AL-FARABI KAZAKH NATIONAL UNIVERSITY

Faculty of Chemistry and Chemical Technology

Education program in the specialty «6D074000 Nanomaterials and Nanotechnology»

|  | Approved at the session of Scientific Council of the faculty protocol № 11 «25 » 06 2015 Dean of the faculty___________________ Dr. of Chem. Sci., prof. Ye. K. Ongarbayev |
| --- | --- |

SILLABUS

Elective disciplines module

Elective module 1

NOBA A 8301 «Formation of fullerene and nanostructure at combustion of hydrocarbons»

Second year PhD-course, English division, Fall semester, 3 credits

###### Lecturer’s Full Name:  Mansurov Zulkhair Aymukametovich

Mobile phone:  8701 111 59 83

E-mail:  zmansurov@kaznu.kz

Room faculty of chemistry and chemico-technological 122

DATA module:

The goal of this course:

the study of formation of fullerene and nanostructure at combustion of hydrocarbons.

The objectives of discipline:

- to formation of fullerene at combustion of hydrocarbons;

- to formation of carbon nanotubes at combustion of hydrocarbons;

- to formation of superhydrohobic soot at combustion of hydrocarbons;

- to formation of graphene at combustion of hydrocarbons.

The study of the course is based on materials covered in such prerequisite disciplines as "Quantum Chemistry", "Physical Chemistry", "Organic Chemistry", and is in close connection with the following disciplines: "Chemical Physics", "Solid State Chemistry", "Physico-chemical Methods of Analysis", "Material Science" and "Nanotechnology ".

Upon completion of this course, the students should:

have an idea of:

- the combustion method of producing fullerene and nanostructure.

know:

- to formation of fullerene at combustion of hydrocarbons;

- to formation of carbon nanotubes at combustion of hydrocarbons;

- to formation of superhydrohobic soot at combustion of hydrocarbons.

Prerequisites: "Quantum Chemistry", "Physical Chemistry", "Organic Chemistry", "Physicochemical Methods of Analysis", "Chemical Physics"

Post-requisites: "Solid State Chemistry", “Material Science” and “Nanotechnology”

STRUCTURE, SCOPE AND CONTENT OF DISCIPLINE

| Weeks | Name of the subject | hours | Max balls |
| --- | --- | --- | --- |
| 1 | Lecture 1. Introduction. Formation of nanomaterials in combustion of hydrocarbons | 1 |  |
|  | Seminar 1. Formation of nanomaterials in combustion of acetylene-oxygen flame |  | 10 |
| 2 | Lecture 2. Advantage of the method synthesis of nanomaterials in flame | 1 |  |
|  | Seminar 2. Formation of nanomaterials in combustion of methane-oxygen flame |  | 10 |
| 3 | Lecture 3. Synthesis of fullerenes in flame | 1 |  |
|  | Seminar 3. Formation of nanomaterials in combustion of propane-oxygen flame |  | 10 |
|  | IWTS 3. Methods of investigation of fullerene obtained by flame |  | 15 |
| 4 | Lecture 4. Synthesis of fullerenes under the conditions of combustion of a benzene–oxygen–argon mixture at a low pressure in an electric field | 1 |  |
|  | Seminar 4. Formation of nanomaterials in combustion of butane-oxygen flame |  | 10 |
| 5 | Lecture 5. Synthesis of carbon nanotubes in premixed, laminar flame | 1 |  |
|  | Seminar 5. Formation of nanomaterials in combustion of mixture of the propane-butane oxygen flame |  | 10 |
|  | IWTS 5. Methods of investigation of carbon nanotubes obtained by flame |  | 15 |
| 6 | Lecture 6. Controlling MWNT growth in flames | 1 |  |
|  | Seminar 6. Formation of nanomaterials in combustion of benzene-oxygen-argon flame |  | 10 |
| 7 | Lecture 7. Synthesis single-walled carbon nanotubes in flame | 1 |  |
|  | Seminar 7. Formation of nanomaterials in combustion of mixture of the propane-benzene-oxygen-argon flame |  | 10 |
|  | Landmark control |  | 100 |
|  | Midterm |  | 100 |
| 8 | Lecture 8. Mechanism of soot formation and nanostructure in rich fuel | 1 |  |
|  | Seminar 8. Type of the mechanism of soot formation and nanostructure in rich fuel |  | 10 |
| 9 | Lecture 9. Obtaining hydrophobic soot with iron nanoparticles in propane flame | 1 |  |
|  | Seminar 9. Synthesis of hydrophobic soot in flame |  | 10 |
|  | IWTS 9. Methods of investigation of hydrophobic soot obtained by flame |  | 15 |
| 10 | Lecture 10. Synthesis of hydrophobic soot in hydrocarbon (laminar, premixed) flame | 1 |  |
|  | Seminar 10. Formation of graphene in combustion of mixture of the propane-oxygen-argon flame |  | 10 |
| 11 | Lecture 11. Synthesis of graphene layers in a hydrocarbon flame | 1 |  |
|  | Seminar 11. Formation of graphene in combustion of mixture of the butane-oxygen-argon flame |  | 10 |
|  | IWTS 11. Methods of investigation of graphene obtained by flame |  | 15 |
| 12 | Lecture 12. Synthesis of graphene layers in the dual flame | 1 |  |
|  | Seminar 12. Formation of graphene in combustion of mixture of the benzene-oxygen-argon flame |  | 10 |
| 13 | Lecture 13. Synthesis of graphene layers in the diffusion back flame | 1 |  |
|  | Seminar 13. Formation of graphene in combustion of mixture of the ethelyne-benzene-oxygen-argon flame |  | 10 |
| 14 | Lecture 14. Synthesis of graphene at low pressure in laminar flame | 1 |  |
|  | Seminar 14. Formation of graphene in combustion of mixture of the propane-benzene-oxygen-argon flame |  | 10 |
|  | Landmark control |  | 100 |
|  | Midterm |  | 100 |
|  | Total |  | 400 |

Key concepts in the discipline of knowledge and competence: nanotechnology, nanotubes, fullerenes, the hydrophobic carbon black, soot particles, the synthesis of nanoparticles, waterproofing materials, the impact of the electric field, the structure of the nanoparticles, the chemical properties of nanoparticles.

References for students individual assignments

- Z.A. Mansurov. Soot formation. – Almaty, Kazakh University, 2015, P. 167

- З.А. Мансуров, Н.Г. Приходько, А.В. Савельев. Образование ПЦАУ,фуллеренов, углеродных нанотрубок и сажи. – Aлматы «Қазақ университеті» 2012, 379 бет.

- Л.Н. Сидоров, М.А. Юровская, А.Я. Борщевский, И.В. Трушков, И.Н. Иоффе. Фуллерены: Учебное пособие изд. «Экзамен», 2005, 688 с.

- П.Н. Дьячков. Углеродные нанотрубки. – М.: БИНОМ. 2006, 293 стр.

- A. Jorio, G. Dresselhaus, M.S. Dresselhaus. Carbon Nanotubes Advanced Topics in the Synthesis, Structure, Properties and Applications// Springer. 2013

- Z.A. Mansurov, M. Nazhipkyzy, B.T. Lesbayev, N.G. Prikhodko, M. Auyelkhankyzy, I.K. Puri. Synthesis of superhydrophobic carbon surface during combustion propane// Eurasian chemico-technological journal. 2012. V. 14: 1 P. 19-23

- S. Naha, S. Senb, I.K. Puri. Flame synthesis of superhydrophobic amorphous carbon surfaces// Letters to the Editor / Carbon 45 (2007) 1696–1716

- Mansurov Z.A., Prikhodko N.G., Auyelkhankyzy M., Lesbayev B.T., Nazhipkyzy М Synthesis of Single and Few Layer Graphenes in Flames // 7th European Combustion Meeting 2015. – Budapest, Hungary, 2015, P. 118-119.

- Prikhodko N.G., Mansurov Z.A., Auyelkhankyzy M., Lesbayev B.T., Nazhipkyzy M., Smagulova G.T. Flame synthesis of graphene layers at low pressure// Khimicheskaya Fizika, 2015, Vol. 34, No. 9, pp. 68–73.

The policy rate
Requirements on students: mandatory attendance, activity during the lectures and practical classes, homework, the implementation of TSS and job training to employment.
Unacceptable: delay, withdrawal from classes, the use of cell phones during school hours and delayed delivery jobs without good cause.
Control forms of knowledge:
Quizzes (test papers): 5 work in the semester

Individual Job (SRD): 10 jobs in the semester

Final exam: during the examination session
The criteria for assessment, scores in%
Control Work 					30
Individual tasks (SRD) 			30

Final Exam 					40

Scale of assessment of knowledge:

| Letter grade | Grade point Value (GPA) | Percent range | Description |
| --- | --- | --- | --- |
| А | 4.0 | 95-100 | Excellent |
| А- | 3.67 | 90-94 |  |
| В+ | 3.33 | 85-89 | Good |
| В | 3.0 | 80-84 |  |
| В- | 2.67 | 75-79 |  |
| С+ | 2.33 | 70-74 | Satisfactory |
| С | 2.0 | 65-69 |  |
| С- | 1.67 | 60-64 |  |
| D+ | 1.33 | 55-59 |  |
| D | 1.0 | 50-54 |  |
| F | 0-49 |  | “Failure”-unsatisfactory |
| Р | - | 0-60 65-100 | " Pass " (not included in the calculation of GPA) |
| NP | - | 0-29 0-64 | “No Pass " (not included in the calculation of GPA) |
| W | - | - | " Withdrawal " (not included when calculating GPA) |
| AW |  |  | "Academic Withdrawal " for academic reasons (not included when calculating GPA) |
| AU | - | - | " Audit” (not included when calculating GPA) |

In assessing student work during the semester account, the following is taken into:
- Attendance
- The active and productive participation in practical exercises
- Learn the basic and further reading
- Homework
- Implementation of CDS
- Timely delivery of all jobs (for the late delivery of the three SES rating of AW)
The policy of academic conduct and ethics

Be tolerant and respect opinions of others. Objection is formulated in the correct the form. Plagiarism and other forms of cheating are not allowed. Unacceptable prompting and cheating during the delivery of the CDS, and intermediate control final exam, copying problems solved by others, for exam another student. The student, caught in the rigging of any information rate receive a final rating of «F». Help: For advice on the implementation of independent work (CPC), their delivery and protection, as well as additional information passed material and all other emerging issues for teaches courses please contact the teacher in IWDT period.

Considered at the meeting 		record number from	"    "________2015

Head of the Chair  ________________________M.I.Tulepov

(signature)

Lecturer						Z.A.Mansurov